## Slide 1: Cast Iron
Ferrous alloys with > 2.1 wt% C
  more commonly 3 - 4.5 wt%C
low melting (also brittle) so easiest to cast
Cementite decomposes to ferrite + graphite
  Fe3C  3 Fe () + C (graphite)
  generally a slow process
Notes:   So phase diagram for this system is different (Fig 12.4)

## Slide 2: Fe-C True Equilibrium Diagram
Graphite formation promoted by
Si > 1 wt%
slow cooling
From Fig. 9.2
Callister’s Materials Science and Engineering, Adapted Version.
(Fig. 9.2 adapted from Binary Alloy Phase Diagrams, 2nd ed.,
Vol. 1, T.B. Massalski (Ed.-in-Chief), ASM International, Materials Park, OH, 1990.)
1600
1400
1200
1000
800
600
400
0
1
2
3
4
90
L
g
+L
 + Graphite
Liquid +
Graphite
(Fe)
Co , wt% C
0.65
740°C
T(°C)
 + Graphite
100
1153°C
g
Austenite
4.2 wt% C
a + g
Notes: Cast irons have graphite

## Slide 3: Types of Cast Iron
Gray iron
graphite flakes
weak & brittle under tension
stronger under compression
excellent vibrational dampening
wear resistant
Ductile iron
add Mg or Ce
graphite in nodules not flakes
matrix often pearlite - better ductility
From Fig. 9.3(a) & (b), Callister’s MSE, Adapted Version.

## Slide 4: Types of Cast Iron
White iron
<1wt% Si so harder but brittle
more cementite
Malleable iron
heat treat at 800-900ºC
graphite in rosettes
more ductile
From Fig. 9.3(c) & (d), Callister’s MSE, Adapted Version.